###### Rockpanel Woods

A Rockpanel board surface treated with a triple layer water based coating available in a range of 17 standard wood grain finishes.

The surface has excellent UV resistance when tested in accordance with ISO 4893-1&2 and judged in accordance with ISO 105-A02 and ISO 105-A03.

Board dimensions: 3050 x 1200mm

Board thickness: 8 mm

Available in a choice of durable for general applications or Xtreme for applications where greater mechanical strength is required.

Protect plus finish is standard which improves UV protection and provides anti-graffiti and self-cleaning finish.

All Rockpanel standard products have a maximum lead time of 2 weeks.

Rockpanel Woods has been awarded with several ETA certificates.

Please consult Rockpanel BV for advice on use of other Rockpanel Wood’s cladding products in non-ventilated constructions.

(Please delete clauses in red to suit specification)

950 FASCIAS/BARGES/SOFFITS: PRE-FINISHED STONEWOOL BOARD:

Product reference:

Rockpanel Woods Durable board

Rockpanel Woods  Xtreme board

Material:	Compressed Rockwool with thermo-hardening synthetic binding     compounds

Manufacturer: Rockwool BV / Lapinus, Industrieweg 15

6045 JG Roermond, The Netherlands

Sales Representative: Rockwool BV / Group Rockpanel, Wern Tarw, Pencoed, Bridgend CF35 6NY.  Tel:01656 863210.  Fax: 01656 863611.    E-mail: info@rockpanel.co.uk.  Web: www.rockpanel.co.uk.

Thickness: 8mm

Finish: Protect Plus as standard

Colours:

Cherry / Teak / Oak / Maple / Mahogany / Beech / Alder / Merbau / Rhinestone Oak / Ceramic Oak / Marble Oak / Slate Oak / Carbon Oak /

Ebony Slate / Ebony Granite / Ebony Marble / Ebony Limestone

# Fixings:

# Rockpanel Torx screw:

Stainless steel torx head A1S1 316 grade 4.5x35mm screws, according ETA approval with colour matched heads.

Rockpanel ring shank nail:

Ring shank A1S1 316 grade stainless steel 2.7/2.9 x32 mm (flat head) nails, according ETA approval with colour matched heads.

.

Number and location:

8mm boards

Torx head screws fixed at maximum spans of 600mm and 600mm vertical centres.

Nails to be fixed at maximum spans of 600mm and 400mm vertical

centres.

Please consult Rockpanel BV for wind loading calculations Fixings to be positioned minimum 15mm from the vertical edge of the board and minimum 50mm from the horizontal edge of the board.

Joints

Type/treatment:

Vertical joint treatment

Flexible Joint Gasket weather and UV resistance at vertical board joints (for example ref: 090/60P of Plastestrip)

Colour: Black

Flexible Joint Gasket weather and UV resistance at intermediate supports (for example ref: 090/36P of Plastestrip)

Colour: Black

Flexible Joint Gasket weather and UV resistance at vertical corner joints (for example ref: 090/75P of Plastestrip)

Colour: Black

Optional:

Soffit strip ventilator for 10,000 MM² /M Air Flow for example Ref:055/10K

Colour: Colour matched to board / Black / White

Soffit strip ventilator for 25,000 MM² /M Air Flow    for example Ref:085/25L

Colour: Colour matched to board / Black / White.

Manufacturer/ Distributor: Plastestrip (Profiles) Ltd, Trenance Mill, St Austell, Cornwall, PL25 5LZ. Tel:

01726 74771. Fax: 01726 69238.

E-mail: sales@plastestrip.com Web: www.plastestrip.com

Other requirements:

No gaskets required on sofft boards, providing fascia board extends 7.5mm beyond the soffit board.

Construction: Rockpanel Woods can be used in ventilated and non-ventilated constructions. For use in non-ventilated constructions, please contact Rockwool BV / Rockpanel group for advice.

Board joints:	Fascias & soffits – Maintain a 5mm gap on all vertical joints.

Maintain a gap of 5mm between the junction of the soffit board and the fascia board.

Junction of Soffit and Wall: Maintain a 5mm gap between end of soffit board and external wall face.

Support:

50mm x 38mm softwood timber at maximum 600mm centres with 75 x 38mm timber at vertical board joints.  All timber to be treated to Clause G20 270

270 Ungraded Softwood for Fascia, Soffit and Barge supports.

- Quality of timber: free from decay, insect attack (except pinhole borers) and with no knots wider than half the width of the section.

- Surface finish: PSE

- Treatment: C2