# Rockpanel® Colour

A Rockpanel surface treated with four layers water-based acrylic coating, available in a range of 20 standard colours with any RAL or NCS colour available to order (subject to minimum quantity).  The surface has excellent UV resistance when tested in accordance with TR010 and judged in accordance with EN 20105-A02.

Board dimensions:	3050 x 1200mm (2500 x 1200mm) available in some colours)

Board thickness:  8 mm (Durable and Xtreme) or 9 mm (FS Xtra)

Available in a choice of durable – for general applications, Xtreme – for applications where greater mechanical strength is required and suitable for ground level installations or FS Xtra - in case a non-combustible board is required.

Each has the option of Protect Plus finish.  The finish improves UV protection and provides an anti graffiti finish.  The Protect Plus finish requires a minimum order quantity of 100m2 and a six week lead time.  All standard Rockpanel products have a maximum lead time of 2 weeks.

Rockpanel Colour has been awarded with an European Technical Approval: ETA 07/0141 for Durable Quality and ETA 12/0054 for Xtreme quality

Rockpanel Colour can be used in ventilated and non-ventilated constructions. For use in non-ventilated constructions, please contact ROCKWOOL BV / Rockpanel Group for advice.

(Please delete clauses in red to suit specification)

150 RIGID SHEET CLADDING....

Product reference:

Rockpanel Colour Durable board

Rockpanel Colour Xtreme board

Rockpanel Colour FS Xtra board

Material:	    Inert ROCKWOOL panels with pre-finished decorative coating

Manufacturer; ROCKWOOL BV / Lapinus, Industrieweg 15, 6045 JG Roermond, The Netherlands.

Sales Representative; ROCKWOOL BV / Rockpanel Group, Wern Tarw, Pencoed, Bridgend CF35 6NY.  Tel:01656 863210.  Fax: 01656 863611.

E-mail: info@rockpanel.co.uk.  Web: www.rockpanel.co.uk.

Thickness:  	   	8 mm for Durable Board

8 mm for Xtreme Board

9 mm for FS Xtra Board

Finish:              Standard finish/Protect Plus Finish

Colours:        Pure White RAL 9010 / Oyster White RAL 1013/

Cream/White RAL 9001/ Light Ivory RAL 1015 /

Purple Red RAL 3004/Fir Green RAL 6009 /  Light Grey RAL 7035 / Signal Grey RAL 7004 / Blue Grey RAL 7031 /Anthracite Grey RAL 7016 / Black Grey RAL 7021 / Jet Black  RAL 9005 / RAL 5011 Steel Blue /Terra Brown RAL 8028 / Silver Grey RAL 7001 / Dusty Grey RAL 7037 / Stone Grey RAL 7030 / Umbra Grey RAL 7022 / oxide Red RAL 3009 / Black Red RAL 3007.

Fire Classification according EN 13501-1:

Rockpanel Colour Durable board providing B-s2,d0

Rockpanel Colour Xtreme board providing B-s2,d0

Rockpanel Colour FS Xtra board providing A2-s1,d0

# Fixings for Aluminium:

# Aluminium (AlMg5)Rivet with colour match head minimum Ø 14mm, length 18 mm and shank diameter 5 mm.	Pre-drill Rockpanel with 8 mm holes and 5.2 mm for centre fixings.  A spacer tool should be used when fixing rivets.

# Ref:RP/fix 20 Stainless steel (A4 grade) self tapping screws (thickness aluminium between 1,2 and 2,5 mm) with colour matched heads. Please note when using self tappers the maximum panel size is 1500 x 1200mm.

# Fixings for steel:

# Ref:RP/fix 20 Stainless steel (A4 grade) self tapping screws with colour matched heads.

Ref:	River/spacer tool

Manufacturer:       Plastestrip (Profiles) Ltd, Trenance Mill, St Austell, Cornwall, PL25 5LZ. Tel: 01726 74771. Fax: 01726 69238.

E-mail: sales@plastestrip.com Web: www.plastestrip.com

Number and location:

8mm boards 	Rivets and self-tappers to be fixed at a maximum span of 600 mm and maximum 600 mm vertical centres.

9mm boards 	Rivets and self-tappers to be fixed at a maximum span of 600 mm and maximum 600 mm vertical centres.

Please consult ROCKWOOL BV / Rockpanel Group for wind loading calculations Fixings to be positioned minimum 15 mm from the vertical edge of the board and minimum 50mm from the horizontal edge of the board.

Joints

Type/treatment:

Vertical joint treatment

If desired, blackout tape can be applied to prevent light reflection from aluminium supports.

### Horizontal joint treatment

Rockpanel profile A:

- Aluminium horizontal chair section (with high back) for 8 mm boards

- Aluminium horizontal chair section (with high back) for 10 mm boards in the event of 9 mm FS Xtra

Rockpanel profile B: Aluminium horizontal V-bird section

### External Corner Treatment

Rockpanel profile D:

- External corner profile (aluminium) for 8 mm boards

- External corner profile (aluminium) for 10 mm boards in the event of 9 mm FS Xtra

Rockpanel profile E:

- External capped corner profile (aluminium) for 8 mm boards

- External capped corner profile (aluminium) for 10 mm in the event of 9 mm FS Xtra

Colour		Colour matched to board/Black/White

Distance between boards: > 5 mm

Air gap:  Minimum 20 mm

Consult Rockpanel Group for recommendations and details if designing to NHBC requirements

Secondary support system/framing system;

For example:

Product reference:	Plastestrip Top Hat and Z profile system

Material:		Aluminium

26mm cavity

Ref: AL/TH/26/50		Top Hat Profile

Ref:AL/Z/26/50/26	Z profile

40mm cavity

Ref: AL/TH/40/55		Top Hat Profile

Ref:AL/Z/40/55/26	Z profile

#### Fixings: number and location

Consult with Plastestrip for recommendations and details

For cavities greater than 40mm – 270mm contact Plastestrip for further details

Manufacturer:       Plastestrip (Profiles) Ltd, Trenance Mill, St Austell, Cornwall, PL25 5LZ. Tel: 01726 74771. Fax: 01726 69238.

E-mail: sales@plastestrip.com Web: www.plastestrip.com

Thermal Insulation		As clause 775

Breather membrane:	As clause 785

Rockpanel Accessories:

### Bottom Drips

Rockpanel profile J:	aluminium bottom drip profile

General Accessories:

Accessories:

Ventilated profiles:

Ref: 025/10K	bottom vent strip – 25mm cavity

Ref: 065/10K	bottom vent strip – from 40-65mm cavities

Ref: 090/25K	bottom vent strip – from 65-90mm cavities

Ref: 125/25K	bottom vent strip – from 90-125mm cavities

Manufacturer:       Plastestrip (Profiles) Ltd, Trenance Mill, St Austell, Cornwall, PL25 5LZ. Tel: 01726 74771. Fax: 01726 69238.

E-mail: sales@plastestrip.com Web: www.plastestrip.com

# GENERAL REQUIREMENTS

- CONTROL SAMPLES

- General: Complete an area of the cladding and obtain

approval of appearance before proceeding.

  - Location :...

  - Extent of area...

- FIXING SHEETS

- General: Secure to supports without producing distortion.

- Fasteners: Evenly spaced in straight lines, in pairs across

joints and sufficient distance from edge of sheet to prevent

damage.

- COVER STRIPS

- General: Form straight runs in single lengths wherever possible

- Location and method of forming joints: Submit proposals where

not detailed.

Due to temporary increase of requirement for technical advice, there is a delay in answering your E-mail and/or question.

In case of any urgency you can contact personally